## Slide 1: Design Rules Summary
for Drawing Layers
2026/04/20

## Slide 2
Drawing Layer Table

## Slide 3
Cat-1: Prohibited
AP
WN
WN
AR
AP
AC
AP+AN
+AC+AR
+GC+GR
M1
M1
M2
CO
V1
Function: Wmin/max: L1 Width min/max
Smin/max: L1 Space min/max (L1=L2)
Smin/max: L1 Separate L2 min/max
Emin/max: L1 Enclosed L2 min/max
Fmin/max: L1 Enclosing L2 min/max
ECmin: MOS Endcap min
Wfix: L1 Windth equal
Sfix: Space equal
Donut: L1 Souuounded by L2
None: Not Exist
M1
M2
PO
PO
V1(P)
V1(P)：V1 on PE
Rule | L1 | L2 | Func | MIN | MAX
WN.Z1 | WN(R) | AP | None | 0.0 | 
WN.Z2 | WN(C) | AP | None | 0.0 | 
WN.Z3 | WN(C) | AR | None | 0.0 | 
CO.Z1 | CO | AA+GC+GR | None | 0.0 | 
CO.Z3 | CO | M1 | None | 0.0 | 
V1.Z1 | V1 | M1 | None | 0.0 | 
V1.Z2 | V1 | M2 | None | 0.0 | 
PO.Z1 | PO | M1 | None | 0.0 | 
PO.Z2 | PO | M2 | None | 0.0 | 
PO.Z3 | PO | V1(P) | Exist | 0.0 | 
WN
AC
AR

## Slide 4
AR
AN
WN.S2
AN.WR
AR.AN
AR.S1
WN
(C)
AN.WC
AC.AN
AP
WN.S4
AC
AR
WN.S5
WN.S6
WN.S3
AC.W1
AR.WR
AC.WC
AC.S1
WN.W1
WN.S1
AP
AN
AN
AP
WN
(C)
WN
(R)
WN
(R)
AN
AP
AN
WN.AN
AP
WN.AP
WN
WN
WN.AN
WN.AP
WN.AN
WN.AP
Cat-2: WN to AP/AN/AR/AC related
AN
AC.GC
AC
Rule | L1 | L2 | Func | MIN | MAX
WN.W1 | WN |  | Wmin | 8.0 | 
WN.S1 | WN | WN | Smin | 12.0 | 
WN.S2 | WN | WN(R) | Smin | 9.5 | 
WN.S3 | WN | WN(C) | Smin | 12.0 | 
WN.S4 | WN(R) | WN(C) | Smin | 9.5 | 
WN.S5 | WN(R) | WN(R) | Smin | 8.0 | 
WN.S6 | WN(C) | WN(C) | Smin | 12.0 | 
WN.AP | WN | AP | Smin | 5.0 | 
WN.AN | WN | AN | Smin | 10.0 | 
AR.S1 | AR | AR | Smin | 4.0 | 
AR.WR | AR | WN(R) | Emin | 10.0 | 
AN.WR | AN | WN(R) | Emin | 5.0 | 
AR.AN | AR | AN | Smin | 4.0 | 
AC.W1 | AC |  | Wmin/max | 28.5 | 120.0
AC.S1 | AC | AC | Smin | ??? | ???
AC.WC | AC | WN(C) | Emin | ??? | ???
AN.WC | AN | WN(C) | Emin | 3.0 | 
AC.AN | AC | AN | Smin | 2.8 | 
AC.GC | AC | GC | Emin | 1.4 | 
AC.R1 | AC | AN(C) | Donut | 0.0 | 
WN(R)：WN overlapped AR
WN(C)：WN overlapped AC
AN(C)：AN in WN(C)

## Slide 5
WN
AP
(M)
AN
(M)
AP
AN.S1
AP.W1
AN.AP
AP.S1
DN.AN
AN.WM
AN.S1
GC
AN
AN.W1
AP.WM
DP.AP
AP.AN
AP.S1
DN.S1
AP
(D)
DP.W1
DP.S1
DN.W1
AN
(D)
Cat-3: MOS transistor related
AN
DP.AN
AP
DN.AP
AP.LM
AN.LM
AP.WN
AP.WN
AN.WN
AN(M)：AN-DN
AP(M)：AP-DP
WN(M)：WN overlapped AN/AP
Rule | L1 | L2 | Func | MIN | MAX
AP.W1 | AP |  | Wmin | 1.4 | 
AP.S1 | AP | AP | Smin | 1.4 | 
AP.AN | AP | AN | Smin | 2.8 | 
AP.WM | PMOS | AP-GC | Wmin/max | 3.4 | 60.0
AP.LM | PMOS | GC-AN | Lmin/max | 1.0 | 30.0
AP.WN | AP | WN | Emin | 7.0 | 
DP.W1 | DP |  | Wmin | 2.8 | 
DP.S1 | DP | DP | Smin | 1.4 | 
DP.AP | DP | AP(M) | Smin | 2.8 | 
DP.AN | DP | AN | Smin | 2.8 | 
AN.W1 | AN |  | Wmin | 1.4 | 
AN.S1 | AN | AN | Smin | 1.4 | 
AN.AP | AN | AP | Smin | 2.8 | 
AN.WM | NMOS | AN-GC | Wmin/max | 3.4 | 60.0
AN.LM | NMOS | GC-AN | Lmin/max | 1.0 | 30.0
AN.WN | AN | WN(M) | Emin | 5.0 | 
DN.W1 | DN |  | Wmin | 2.8 | 
DN.S1 | DN | DN | Smin | 1.4 | 
DN.AP | DN | AP | Smin | 2.8 | 
DN.AN | DN | AN(M) | Smin | 2.8 | 

## Slide 6
AP
AN
AP
GC
AN
GC.EP
CO.W1
CO.S1
CO.AN
CO.S1
CO.AP
CO.W1
CO.GG
CO.W1
CO.S1
CO.AP
CO.S1
CO.AN
CO.W1
CO.GG
GC.EN
CO.W1
CO.GC
CO.S1
GC.AP
GC.AN
GC.S1
GC.W1
AP
(D)
AN
(D)
CO.WD
CO.AD
CO.WD
CO.AD
WN
Cat-4: Contact and Poly related
CO(D)
GC(G)
AP(D)：AP not interacted GC
AN(D)：AN not interacted GC
CO(D)：CO on AP(D)/AN(D)
GC(G)：GC for PMOS/NMOS
Rule | L1 | L2 | Func | MIN | MAX
GC.W1 | GC |  | Wmin | 1.0 | 
GC.S1 | GC | GC | Smin | 1.2 | 
GC.AP | GC | AP | Smin | 0.4 | 
GC.AN | GC | AN | Smin | 0.4 | 
GC.EP | PMOS | GC | ECmin | 1.2 | 
GC.EN | NMOS | GC | ECmin | 1.2 | 
CO.W1 | CO |  | Wmin | 1.0 | 
CO.S1 | CO | CO | Smin | 1.0 | 
CO.WD | CO(D) |  | Wfix | 1.2 | 
CO.AD | CO(D) | AP+AN | Emin | 1.2 | 
CO.AP | CO | AP | Emin | 0.8 | 
CO.AN | CO | AN | Emin | 0.8 | 
CO.GG | CO | GC(G) | Smin | 1.0 | 
CO.GC | CO | GC+GR | Emin | 0.8 | 
GC(G)

## Slide 7
WN(R)
AR
WN
(C)
AC
AN
GC.AN
AR.GC
AR.PW
AN
CC.AN
CC.W1
CC.S1
CC.W1
CC.S1
CC.AC
GC(AR)
GC
(R)
GR.W1
GR.S1
GC
(R)
Cat-5: Resistor(AR/RS) and Capacitor(AC) related
AR
AR.XY
CR.AT
CR.W1
CR.AS
AR.XY
CR.W2
GR.L1
AR.L1
AR.W1
CO(RR)
CL(RR)
RS
RR
R.Effective region
Rule | L1 | L2 | Func | MIN | MAX
AR.W1 | RR | RR(L) | Wmin/max | 2.8 | 20.0
AR.L1 | RR | RR(W) | Lmin/max | 13.0 | 100.0
AR.GC | GC | AR | Smin | 1.0 | 
AR.PW | GC(AR) |  | Wmin | 2.0 | 
AR.XY | AR | Bevel | XYmin | 1.0 | 
GC.AN | GC(AR) | AN | Smin | ??? | ???
GC.R1 | AR | GC(AR) | Donut | 0.0 | 
GC.R2 | GC | TieDown |  | 0.0 | 
GR.W1 | RS | RS(L) | Wmin/max | 4.0 | 20.0
GR.L1 | RS | RS(W) | Lmin/max | 20.0 | 100.0
GR.S1 | RS | RS | Smin | 2.0 | 
CR.W1 | CO(RR) |  | Wmin | 1.0 | 
CR.W2 | CL(RR) |  | Wmin/max | 1.0 | 97.5
CR.AT | CO(RR) | AR(T) | Emin | 1.5 | 
CR.AS | CO(RR) | AR(S) | Emin | 1.0 | 
CC.W1 | CO(C) |  | Wmin | 1.2 | 
CC.S1 | CO(C) | CO(C) | Smin | 1.2 | 
CC.AC | CO(C) | AC | Emin | 2.9 | 
CC.AN | CO(C) | AN | Emin | 1.2 | 
GC(AR)：GC in WN(R)
RS(L) ：Length of AR effective
RS(W) ：Width of AR effective
CO(RR)：CO short side on AR
CL(RR)：CO large side on AR
AR(T) ：AR top fringe
AR(S) ：AR side fringe
CO(C) ：CO on AC

## Slide 8
V1.W1
V1.S1
V1.M1
M1
M1.W1
M1.S1
M1
M2
M2
M2.W1
M2.S1
M2.V1
GC
V1.CO
V1.GC
M1
V1.CL
M1.W2
M1(W)
M1.S2
Cat-6: M1/V1/M2 related
M1.CO
AC
M1.CC
M1.SC
M1.CL
M1(C)
CO(S)
CO(L)
CO(C)
Rule | L1 | L2 | Func | MIN | MAX
M1.W1 | M1 |  | Wmin | 1.8 | 
M1.S1 | M1 | M1 | Smin | 1.4 | 
M1.SC | M1(C) | M1(C) | Smin | 10.0 | 
M1.CO | M1 | CO(S) | Fmin | 0.8 | 
M1.CC | M1 | CO(C) | Fmin | 1.2 | 
M1.CL | M1 | CO(L) | Fmin | 1.2 | 
M1.SW | M1(W) | M1 | Smin | 2.0 | 
V1.W1 | V1 |  | Wfix | 1.4 | 
V1.S1 | V1 | V1 | Smin | 1.5 | 
V1.M1 | V1 | M1 | Emin | 1.0 | 
V1.GC | V1 | GC | Smin | 1.2 | 
V1.CO | V1 | CO | Smin | 1.0 | 
V1.CL | V1 | CO(L) | Smin | 1.4 | 
M2.W1 | M2 |  | Wmin | 3.0 | 
M2.S1 | M2 | M2 | Smin | 2.0 | 
M2.V1 | M2 | V1 | Fmin | 1.0 | 
M1(C)：M1 in WN(C)
CO(C)：CO on AC
CO(S)：CO small contact
CO(L)：CO large contact (only on AR)
M1(W)：Wide M1

## Slide 9
WN
AP
AP
ANE.AP
GC
AN
APE.AN
Cat-7: ESD MOS transistor related
APE.LM
ANE.WM
COE.S1
COE.W1
CSE.GC
APE.WM
COE.S1
COE.W1
CSE.GC
COE.AP
COE.AN
CDE.GC
ANE.LM
CDE.GC
ESD
ANE.XY
ANE.XY
APE.XY
APE.XY
APE.CO
ANE.CO
Rule | L1 | L2 | Func | MIN | MAX
APE.WM | PMOS | AP-GC | Wmin/max | 11.0 | 60.0
APE.LM | PMOS | GC-AN | Lmin/max | 2.0 | 30.0
APE.AN | APE | AN | Smin | 10.0 | 
APE.XY | APE | Bevel | XYmin | 1.4 | 
APE.CO | APE | CO | Smin | 2.0 | 
ANE.WM | NMOS | AN-GC | Wmin/max | 11.0 | 60.0
ANE.LM | NMOS | GC-AN | Lmin/max | 2.0 | 30.0
ANE.AP | ANE | AP | Smin | 10.0 | 
ANE.XY | ANE | Bevel | XYmin | 1.4 | 
ANE.CO | ANE | CO | Smin | 2.0 | 
COE.W1 | CO(E) |  | Wfix | 3.0 | 
COE.S1 | CO(E) |  | Smin | 1.6 | 
CDE.GC | CD(E) | GC | Smin | 7.0 | 
CSE.GC | CS(E) | GC | Smin | 3.0 | 
COE.AP | CO(E) | AP | Emin | 4.0 | 
COE.AN | CO(E) | AN | Emin | 4.0 | 
SOURCE
DRAIN
SOURCE
DRAIN
APE/ANE)：AP/AN on ESD)
CO(E)：CO on ESD

## Slide 10
M1.PO
Cat-8: PAD related
M2(P)
M1(P)
PO
PO
q
q
V1(P)
M2.PO
PO.W1
PO.S1
V1.PO
AA/GC/M1/M2
PO.XX
M1.PE
M2.PE
M2.PW
M1.PW
Rule | L1 | L2 | Func | MIN | MAX
PO.W1 | PO |  | Wmin | 70.0 | 
PO.S1 | PO |  | Smin | 64.0 | 
M2.PO | M2(P) | PO | Fmin | 5.0 | 
M1.PO | M1(P) | PO | Fmin | 5.0 | 
PO.V1 | PO | V1(P) | Emin | 10.0 | 
PO.AP | PO | AP | Smin | 14.0 | 
PO.AN | PO | AN | Smin | 14.0 | 
PO.GC | PO | GC | Smin | 14.0 | 
PO.M1 | PO | M1 | Smin | 14.0 | 
PO.M2 | PO | M2 | Smin | 14.0 | 
M2.PE | M2 | Extention |  | 19.0 | 
M2.PW | M2 | Extention | Wmin | 40.0 | 
M1.PE | M2 | Extention |  | 19.0 | 
M1.PW | M2 | Extention | Wmin | 40.0 | 
** Not yet implemented
M1(P)：M1 on PO
M2(P)：M2 on PO
V1(P)：V1 on PO

## Slide 11: Design Rule cotrol
DRC integrity

## Slide 12: DRC
run.drc
DR_Table.xls
python/*.py
Document
PCell
python/rules_def.py
DRC_summary.ppt
DR_csv2drc.py
DR_csv2py.py
Method
Cut & Paste
# ALL Critical Dimension parameters are referenced by ‘XX.YY’ rule’s name.

## Slide 13: Design to Tapeout Process
Mask Data Preparation

## Slide 14: Designer
TR-1um_USER_Project
TR-1um_MPW_template
Fabrication
OpenSUSI
Tokai Rika
Signoff DRC
TR-1um_MPW_XXX
[clone]
TR-1um_USER_Project
[push]
local
remote
TR-1um_USER_Project
[action]
Precheck
DRC
MDP
[Import artifact]
TR-1um_MPW_XXX
[action]
Logo insertion
Aggregation
DRC
Download GDSII
PCM TEST
Wafer out